Curing Time vs. Strength

| Time | Tensile Strength (psi) |
| --- | --- |
| 1 min | 1140 |
| 2 min | 2980 |
| 3 min | 3410 |
| 5 min | 3980 |
| 10 min | 4410 |
| 20 min | 4690 |
| 30 min | 4980 |
| 40 min | 4980 |
| 50 min | 4980 |
| 60 min | 4980 |
| 24 hours | 4980 |

Test Conditions

- Test specimen……………..  Rigid PVC: 0.5 x 0.5 x 1.5 in

- Surface treatment…………  Polished with smooth-cut file and degreased with methyl chloroform

- Bonding atmosphere………  73.5˚F, 60% RH

- Curing time………………..  24 hours under above atmosphere

- Speed of load………………  20 mm (0.8in)/min

- Adhesive…………………...  Aron Alpha Type 201

- Test method………………..  ASTM D 2095