Impact Strength – 401X vs. 201

|  | Impact Strength (lb•in/in2) |
| --- | --- |
| Adherend | 401X | 201 |
| Stainless Steel | 106 | 28 |
| Steel | 157 | 28 |
| Aluminum | 73 | 34 |
| Copper | 84 | 28 |
| Brass | 73 | 17 |

Test Conditions

- Test specimen……………..  Upside: 0.38 x 1.0 x 1.0 in

Bottom: 0.75 x 1.0 x 1.75 in

- Surface treatment…………  Polished with smooth-cut file and degreased with methyl chloroform

- Bonding atmosphere………  73.5˚F, 60% RH

- Curing Time………………..  24 hours under above atmosphere

- Test Machine………………  TOYO SEIKI Impact Tester

- Impact speed……………….  10.9 ft./sec.

- Test Method………………..  ASTM D 950