Water Resistance (Immersion in Water)

Note: After 24-hour curing, the test specimens were immersed in water.  Then, test specimens were taken out of water at a specified interval to measure the bonding strength.

| Adherend | Tensile Strength (psi) |
| --- | --- |
|  | Before Immersion | After 1 month | After 3 months | After 6 months | After 1 year |
| Rigid PVC | 4980 | 4980 | 4980 | 4980 | 4980 |
| ABS | *3560 | *3560 | *3560 | *3560 | *3560 |
| Phenolic | *4980 | 1420 | 360 | 140 | 0 |
| Neoprene Rubber | *360 | *360 | *360 | *360 | *360 |
| Steel | 4550 | 430 | 210 | 0 | - |
| Copper | 4980 | 4980 | 4980 | 4980 | 4980 |

*Material Failure

Test Conditions

- Test specimen……………..  0.5 x 0.5 x 15 in

- Surface treatment…………  Polished with smooth-cut file and degreased with methyl chloroform

- Bonding atmosphere………  73.5˚F, 60% RH

- Speed of load………………  20 mm (0.8in) /min.

- Water………………………  Stored at room temperature

- Adhesive…………………..  Aron Alpha Type 201

- Test Method………………..  ASTM D 2095